Introduction

1. Urgency of thesis

In Vietnam, deterioration of steel reinforced concrete structures is now alarming, especially in the coastal area with tidal marine water and marine atmosphere. In the coastal region,   it is estimated that about 50% of the reinforced concrete structures are now being eroded and destroyed seriously. Through the survey, in the coastal and marine climates, after 10 to 20 years of operation, many structures appear corrosion of steel that results in cracking or spalling of the concrete. This has changed the structure, reduced bearing capacity of steel, as well as shortened the service-life of the strcuture. Thus, for reinforced concrete structures such as highway bridges, the chloride-induced corrosion of rebar has been a major problem with serious economic and safety implications.

The thesis entitled“Research on rehabilitation of chloride-contaminated reinforced concrete by using ECE and EICI methods” aims to demonstrate the use of ECE and EICI methods to remove chloride ions away from the steel rebarin chloride-contaminated mortar and to mitigate the corrosion of the embedded steel.

2. Contents of study

- Research and determind the suitable parameters of ECE to remove chloride ions away from chloride-contaminated mortar.

- Research on the effect of ECE on elements distribution, corrosion of rebar and compressive strength of cement motars

- Research and determind the suitable parameters of ECE to inject the inhibitor into the chloride-contaminated reinforced mortar.

- Research on the effect of EICI on inhibition efficiency for rebar and compressive strength of cement motars

- Based on the findings from laboratoty, on-site-trial at the coastal area will executed.

3. Scientific findings and novelty of theis

* Scientific findings

- The thesis shows effect of operating parameters (such as electrolytes, current density, time of treatment..) on the effectiveness of ECE and EICI treatments.

- ECE treatment was effective in removing chlorides whenusing both electrolytes. Chloride content was decreased by70% relative to the initial chloride after 4 weeks of treatment. When using a current density of 1 A/m2,the chloride reduction increased with increasing time of treatment.The potentiodynamic weak polarization tests showed that ECE treatment halted chloride-induced corrosion of therebar by passivating it. If a current density of 1 A/m2 was usedduring the ECE, the values of icorr after 4 weeksdecreased by 36 and 34 per cent, respectively.The EIS data revealed that ECE treatment increased theresistivity of the mortar, leading to the formation of a more dense and less permeable microstructure of cement mortars. ECE treatment improved significantly the compressive strength of the mortar..

- After 4-week EICI treatment in NaOH,[TBA+] content was 2.0% and 2.5% by mass ofcement mortar, for uncontaminated and chloridecontaminatedsamples, respectively. The potentiodynamic weak polarization tests showedthat EICI treatment halted chloride-induced corrosionof the rebar. The electromigration test showed that EICI improved the chloride penetration resistanceof the mortar, as indicated by the reduced apparentdiffusion coefficients of chloride anion, by 38%from 1.0 × 10−10 m2/s. EICI treatmentsignificantly improved the compressive strength ofcement mortars.

-	Establish the system and electrolytic storage material for the on-site trial of ECE and EICI methods for chloride contaminated concrete structure at Lan 1- Water gate (ThaiBinh). After 2 weeks ECE, 81,2% chloride content was removed from the position column. After 4 weeks EICI, [TBA+] concentration around rebar reached at the value of 2,2 wt.%. After 1 year (since the disconnection of test), the rebar was still in the passive state under good protection.

* Novelty of thesis

- Study and application of EICI method for injection of corrosion inhibitor into the reinforced structure in Vietnam. The EICI should be used immediately after ECE for better protection of chloride-contaminated reinforced concrete.

- Application of ECE and EICI method to rehabilitate a part of chloride-contaminated reinforced concretestructure at Lan 1- Water gate (ThaiBinh).

4. Structure of thesis

Thesis comprises 112 pages. Introduction: 3 pages; Chapter I: Literature review: 28 pages; Chapter II: Experimentals and methods: 18 pages; Chapter III: Results and discussion: 50 pages; Conclusions: 2 pages; References: 9 pages.

CHAPTER I: Literature REVIEW

Chapter 1 presents a review on the following problems:

- Introduction to steel reinforced concrete

- Overview on corrosion of steel rebar in concrete

- Overview on  corrosion  inhibitors used in reinforced concrete

- Electrochemical methods for protection and rehabilitation of chloride-contaminated reinforced concrete.

CHAPTER II: Experimentals and methods

2.1. Fabrication of steel-reinforced mortar and concrete

Steel rebars were embedded in each salt-contaminatedcement mortar, with a mortar cover of 2.5 cm. (Figure 2.1a). For each sample, the ratio of cement:sand:water:sodium chloride, by weight, was 1:1.75:0.45:0.005. After mixing, the fresh mixture was poured into polypropylene plastic molds to form Ø 100 mm×50 mm cylindrical samples.The steel-reinforced cement mortar specimens were demolded after 24 h and then cured in a wet chamber for 28 days, before being subjected to the electrochemical tests.

| a) | b) |
| --- | --- |

Figure 2.1: Diagram of steel-reinforced mortar (a) and  concrete (b)

2.3. ECE experimental setup

The extraction treatment was performed by using a constantcurrent with 0.1M NaOH or 0.1M Na3BO3as theelectrolyte and stainless-steel 304 mesh as the external anode (Fig.2.2a).The electrical current density delivered on the steel surface was 1 and 5 A/m2. The periods of this application of extraction lasted 1-4 weeks.

## 2.4. ECE experimental setup

The EICI treatment was performedby using a constant currentwith 0.1M NaOH or 0.1MNa3BO3 solutions containing 25mM TBAB as the electrolyteand stainless-steel 304 mesh as the external anode (Fig. 2.2b). Thesolution was replaced every 2 to 3 days to maintain alkalinity.The electrical current density delivered on the steelrod surface was controlled at 5 A/m2. This treatment lastedone to four weeks, based on the experimental design.

| a) | b) |
| --- | --- |

Figure 2.2: Diagram of ECE (a) and EICI (b) treatments

2.5. Free chloride measurement by using thecustomized chloride sensor

Chloride sensors were fabricated using an electrodeposition process. First, the silver wire was immersed in a 0.1M KCl along with a clean graphite rod, connected to the positive and negative terminals of potentiostat. A constant current was applied by the potentiostat to provide a 1 A/m2 current density for 30 min [40]. The quality of these sensors was first examined by reading their electrochemical potential in the 5 aqueous solutions containing known amounts of NaCl. At the end of the ECE treatment (after 2 and 4 weeks), specimens were cut in slices and later powdered. The powder was then screened through a 300-µm sieve, oven-dried at 80°C overnight and cooled to Troom. 10g of dry mortar powder was added into 100 ml of the distilled water, then sonicated for 1 h. The pHof this solution was ~11.

2.6. Chloride permeability of cement mortars: before and after EICI test.

To test the chloride permeabilityof cement mortars, electromigration experiments were performed using the two half-cells as shown in Figure 2.4.Each of the two half-cells containedone platinum electrode, a 20-volt DC electric field was maintainedacross the disc through the two platinum electrodes. The diffusion coefficient 𝐷 of Cl− in cementmortars can be estimated using the following equation.where 𝑧 is charge number, 𝐹 is Faraday constant, 𝑅 is gasconstant, and 𝑇 is absolute temperature, 𝑡0 is time required for the chloride front to penetrate a depth 𝑑 of the specimen [19, 40, 73]:.

2.7. Energy-dispersive X-ray spectroscopy study

The element concentration and profile in cement mortars (beforeand after ECE) were studied using EDX/FESEM. Steel-reinforced cement mortar was cut in cross-slide andthen the mortar surface was coated with a very thin carbonlayer.s. An element was obtained by EDX in 10 mm of mortar adjacent to the reinforcing steel.

Figure 2.4: Experimental setup for electromigration tests

2.8. Quantifying Inhibitor Concentration in Cement Mortars

At the end of EICI, themortar specimens were cut into slices and later powdered.Thepowder was then screened through a 300 𝜇m sieve, ovendriedat 80∘C overnight, and cooled to room temperature. 5 grams of dry mortar powder was added to 50mL of thedistilled water solution and then sonicated for 1 hour beforethe solution was subjected toUV-Vis spectroscopy.By testing four standard alkaline aqueous solutions (pH11) of TBAB (1mM to 20 mM), a calibration curve wasestablished to correlate the optical density at the characteristicpeak and the inhibitor concentration. Thecalibration curve was then used to determine the TBAB concentrationin cement mortar samples after EICI treatments.

## 2.9. Electrochemical characterization of rebar in mortar

## EIS measurements were carried out using the AUTOLAB. The steel rebar was polarized at ±10 mV around its OCP by an alternating current (AC) signal with its frequency ranging from 100 kHz to 100 mHz. In the potentiodynamic weak polarization test, the steel was polarized around its corrosion potential (-30mVto 30 mV/SCE vs OCP) by a direct current signal at a scan rate of 0.2 mV/s. Rp is defined by the slope of the potential current density plot at the corrosion potential. Corrosion current (Icorr) is calculated from Icorr = B/Rp, assuming B = 26 mV for the steel rebar corrosion.

## 2.10. Characterization of compressive strength of mortar

The compressive strength test was carried out by breaking cylindrical mortar specimens (56 mm in diameter and 56 mm in height) in a hydraulic universal testing machine, according to the standard of  TCVN3105:1993 and TCVN 3118:1993.

## Chapter 3:  Results and Discussion

## 3.1. Effect of operating parameters on the efficiency of ECE

## 3.1.2. Effect of current density and electrolyte on the chloride removal

As shown in Fig 3.2, the chloride sensor calibration curve established in such pH11 solutions showed a strong linear correlation between the natural logarithm of the chloride concentration and the chloride sensor potential (Ecl-, vs an Hg/HgSO4 reference electrode). The high R-square value is the excellent reproducibility. After ECE, Fig 3.3 and 3.4 present the reduction in chloride content with time of ECE treatment in sodium hydroxide and sodium borate solutions, respectively. As can be seen in Fig. 3.3, when using the sodium hydroxide solution, the chloride reduction varied with change in current density and duration. The chloride reduction was quite stable (around 70%) when using sodium borate as the electrolyte solution. Similar results were also obtained by other authors, such as 40%-60%  [50] and ~40% [45] or ~ 50% [29] and 21%-78% [75].

# Figure 3.2: Calibration of customized chloride sensors in pH 11

| # (a) | # b) |
| --- | --- |

Figure 3.3: Reduction in chloride content by time of ECE treatment in the sodium hydroxide (a) and  Na3BO3 solutions (b)

## 3.1.3. Effect of current density and electrolyte on the compressive strengh of cement mortar

As indicated from Figures 3.5 and 3.6, ECE treatment can significantly improve the compressive strength the mortar. In comparison to the electrolyte solution, the compressive strengths obtained by treatment in the sodium borate solution were higher than those from the sodium hydroxide solution (up to a 70.5 percent strength increase).

## 3.1.4. Effect of current density and electrolyte on the mortar resistivity

Fig 3.9 and 3.10 present the mortar resistivity before and after ECE treatment in sodium hydroxide and sodium borate solutions, respectively. The mortar resistivity was estimated by the division of |Z| (at frequency of 1.7 KHz) for the thickness of the mortar. It can be observed from these figures that the ECE treatment increased the mortar resistivity. The resistivities of mortar treated in the sodium borate solution were higher than resistance values obtained in the sodium hydroxide solution. Thus, the ECE treatment may lead to a more dense and less permeable microstructure of cement mortars.

| (a) | (b) |
| --- | --- |

Figure 3.5: Compressive strength of cement mortar treated in  the sodium hydroxide (a) and  Na3BO3 solutions (b)

## 3.1.5. Effect of current density and electrolyte on the corrosion behavior of rebar in mortar

Tables 3.2 and 3.3 present the corrosion potential (Ecorr), polarization resistance (Rp) and corrosion current (icorr) values deduced from the weak polarization tests for samples with or without ECE treatment in NaOH and Na3BO3 solutions, respectively. It can be observed from these tables that after ECE treatment, the corrosion potentials of all samples were more positive and it was possible to passivate the steel using this technique, as some authors have suggested.

| (a) | (b) |
| --- | --- |

Figure 3.9: Mortar resistivity before and after ECE treatment in  the sodium hydroxide (a) and  Na3BO3 solutions (b)

Table 3.2: Ecorr,Rp and icorr values of samples with and without ECE treatment in NaOH solution

| Sample (weeks, current density) | Ecorr (V/SCE) | Rp (Ω.cm2) | icorr (mA/cm2) |
| --- | --- | --- | --- |
| 2 wk, 0 A/m2 | -0,278 | 1,23E+05 | 2,11E-04 |
| 2 wk, 1A/m2 | -0,102 | 1,34E+05 | 1,94E-04 |
| 4 wk, 1 A/m2 | -0,175 | 1,92E+05 | 1,36E-04 |
| 2 wk, 5 A/m2 | -0,115 | 1,23E+05 | 2,11E-04 |
| 4 wk, 5 A/m2 | -0,052 | 7,47E+04 | 3,48E-04 |

Table 3.3: Ecorr,Rp and icorr values of samples with and without ECE treatment in Na3BO3 solution

| Sample (weeks, current density) | Ecorr (V/SCE) | Rp (Ω.cm2) | icorr (mA/cm2) |
| --- | --- | --- | --- |
| 2 wk, 0 A/m2 | -0,278 | 1,23E+05 | 2,11E-04 |
| 2 wk, 1A/m2 | -0,248 | 3,88E+04 | 6,70E-04 |
| 4 wk, 1 A/m2 | -0,134 | 1,87E+05 | 1,39E-04 |
| 2 wk, 5 A/m2 | -0,079 | 1,54E+05 | 1,69E-04 |
| 4 wk, 5 A/m2 | -0,08 | 1,39E+05 | 1,87E-04 |

| (a) | (b) |
| --- | --- |

Figure  3.11: Rp values of steel rebar before and after ECE

treatment in  the sodium hydroxide (a) and  Na3BO3 solutions (b)

## 3.1.6. Effect of electrolyte on the morphology and composition of cement mortar

Figure 3.13 shows the SEM images at low and high magnifiction for mortar sample before and after ECE treatment. As shown in this Fig, before ECE the surface of mortar seems porous with lot of pore (Fig 3.13A). After ECE treatemnt, all samples have the compact nd homogenous surface (Figures  3.13B-E). SEM/ EDX data indicated that, the treatment in Na3BO3 solution increased significantly the Ca/Si ratio in the mortar near the rebar when using a current 1 A/m2.

Conclusion of 3.1 part

ECE treatment was effective in removing chlorides whenusing both electrolytes. Chloride content was decreased by70% relative to the initial chloride after 4 weeks of treatment. When using a current density of 1 A/m2,the chloride reduction increased with increasing time oftreatment.The potentiodynamic weak polarization tests showed thatECE treatment halted chloride-induced corrosion of therebar by passivating it. If a current density of 1 A/m2 was usedduring the ECE, the values of icorr after 4 weeksdecreased by 36 and 34%, respectively. EIS data revealed that ECE increased theresistivity of the mortar, leading to the formation of a more dense and less permeable microstructure of cement mortars. ECE treatment improved significantly the compressive strength of the mortar..

Figure 3.13:  SEM images of samples before and after 4 weeks- ECE treatment: A: before ECE, B: NaOH at 1 A/m2,  C: Na3BO3 at5 A/m2, D: NaOH at 1 A/m2,  E: Na3BO3 at 5 A/m2

3.2. Effect of operating parameters on the efficiency of EICI

3.2.2. Effect of electrolyte on the inhibitor content in cement mortar

By testing 5 standard solutions (pH 11) of TBAB (1mM to 20 mM), calibration curve was established to correlate the optical density at characteristic peak (Fig 3.15) and inhibitor concentration. The calibration curve was then used to determine the TBAB concentration in mortar samples after EICI. As shown in Fig 3.16, the calibration curves showed a strong linear correlation between the natural logarithm of the TBAB concentration and optical density.

Fig.  3.15: UV-visible spectra of 5 standard TBAB solutions  pH11.

Fig 3.16: Calibration curve in TBAB solutions at pH 7 and pH11

Table 3.6: [TBA+] content by time of EICI treatment in NaOH

| Samples | After 1 week-EICI test |  | After 4 weeks-EICI test |  |
| --- | --- | --- | --- | --- |
|  | [TBA+] (M) | Wt.% | [TBA+] (M) | Wt.% |
| 0% [Cl-] | 0,0049 | 1,58 | 0,0063 | 2,04 |
| 0,5%[Cl-] | 0,0044 | 1,37 | 0,0080 | 2,54 |

Table 3.7: [TBA+] content by time of EICI treatment in Na3BO3

| Smples | After 1 week-EICI test |  | After 4 weeks-EICI test |  |
| --- | --- | --- | --- | --- |
|  | [TBA+] (M) | Wt.% | [TBA+] (M) | Wt.% |
| 0% [Cl-] | 0,0062 | 2,00 | 0,0087 | 2,76 |
| 0,5%[Cl-] | 0,0068 | 2,20 | 0,0061 | 1,96 |

## 3.2.3. Effect of electrolyte on the compressive strength of mortar

Figures 3.21 and 3.22 shows the compressive strength of two kinds of sample (0% and 0,5% chloride) before and after EICI in NaOH and Na3BO3, respectively. As can be seen in these figures, the EICI treatment improved the compressive strength of the mortar.

| (a) | (b) |
| --- | --- |

Figure 3.21: Compressive strength of cement mortar before and after EICI treatment in NaOH (left) and in Na3BO3   (right)

## 3.2.4. Effect of electrolyte and time of treatment on  corrosion state of rebars

Tables 3.8 and 3.9 present the Ecorr, Rp and icorr values deduced from the linear polarization tests for samples with or without EICI treatment in sodium hydroxide solution, for uncontaminated and contaminated samples, respectively. As can be seen in these tables, the presence of chloride in cement mortar increased significantly the corrosion current of rebar (up to 8.6 times of current increase).

Table 3.8: Ecorr, Rp và icorr values obtained from the linear polarization tests for uncontaminated samples in.NaOH solution

| Time of EICI(weeks) | Ecorr (V/SCE) | Rp (Ω.cm2) | icorr (mA/cm2) | Inhibition efficiency(%) |
| --- | --- | --- | --- | --- |
| 0 | -0,286 | 2,25E+05 | 1,16E-04 | N/A |
| 2 | -0,223 | 1,87E+05 | 1,39E-04 | -19,8 |
| 4 | -0,164 | 2,46E+05 | 1,06E-04 | 8,6 |

Table 3.9: Ecorr, Rp và icorr values obtained from the linear polarization tests for contaminated samples in.NaOH solution

| Time of EICI(weeks) | Ecorr (V/SCE) | Rp (Ω.cm2) | icorr (mA/cm2) | Inhibition efficiency(%) |
| --- | --- | --- | --- | --- |
| 0 | -0,356 | 2,61E+04 | 9,96E-04 | N/A |
| 2 | -0,016 | 2,36E+05 | 2,20E-04 | 77,9 |
| 4 | -0,029 | 1,94E+05 | 2,68E-04 | 73,5 |

Table 3.10: Ecorr, Rp và icorr values obtained from the linear polarization tests for uncontaminated samples in Na3BO3

| Thời gian xử lý(tuần) | Ecorr (V/SCE) | Rp (Ω.cm2) | icorr (mA/cm2) | Inhibition efficiency(%) |
| --- | --- | --- | --- | --- |
| 0 | -0,286 | 2,25E+05 | 1,16E-04 | N/A |
| 2 | -0,079 | 2,42E+05 | 2,14E-04 | 7,6 |
| 4 | -0,138 | 4,53E+05 | 5,74E-05 | 50,9 |

Tables 3.10 and 3.11 present also present the Ecorr, Rp and icorr values deduced from the linear polarization tests for samples with or without EICI treatment in in sodium borate solution, for uncontaminated and contaminated samples, respectively. It can be observed from these tables, after EICI, the corrosion potentials of all samples were more positive and it was  possible to passivate steel.

Table 3.11: Ecorr, Rp và icorr values obtained from the linear polarization tests for contaminated samples in Na3BO3

| Thời gian xử lý(tuần) | Ecorr (V/SCE) | Rp (Ω.cm2) | I corr (mA/cm2) | Inhibition efficiency(%) |
| --- | --- | --- | --- | --- |
| 0 | -0,356 | 2,610E+04 | 9,96E-04 | N/A |
| 2 | -0,066 | 2,43E+05 | 2,14E-04 | 78,5 |
| 4 | -0,055 | 9,15E+04 | 5,68E-04 | 43,0 |

## 3.2.5. Effect of electrolyte on diffusion coefficient of chloride in cement mortar

Figure 3.5 shows the chloride concentrations in the anolyte (destination solution) as a function of time during the electromigration test for mortars with or without EICI treatment. As can be seen in this figure, after EICI treatment in both of the NaOH and Na3BO3 solutions, the value of 𝑡0 increased.

Figure 3.25: Before  EICI: to = 55 mins and  D = 1,0 ×10-10 m2/s;

After EICI in NaOH: to = 125mins; D = 6.2 ×10-11 m2/s; After  EICI

in Na3BO3: to = 96 mins; D = 8,96 ×10-11 m2/s.

| a) | b) |
| --- | --- |
| c) | d) |

Figure 3.26: FESEM images of cementmortars: ((a) and (b)) before EICI treatment; ((c) and (d)) after 4 weeks of EICI treatment. Magnification for (a) to (d): at 5000x (on the left) and at 10000x (on the right)

## Conclusion of 3.2 part

After 4-week EICI treatment in NaOH,[TBA+] content was 2.0% and 2.5% by mass ofcement mortar, for uncontaminated and chloridecontaminatedsamples, respectively. The potentiodynamic weak polarization tests showed that EICI treatment halted chloride-induced corrosionof the rebar. The electromigration test showed that EICI improved the chloride penetration resistanceof the mortar, as indicated by the reduced apparentdiffusion coefficients of chloride anion, by 38% from 1.0 × 10−10 m2/s. EICI treatment significantly improved the compressive strength ofcement mortars.

Transport of ionic and molecular species in mortar is mainly through the pore solution. Thus, by EICI treatment, [TBA+] cations may chemically and physically react with cement hydrates and lead to a less permeable microstructure of cement mortars.The FESEM test revealed that the [TBA+] not only led to denser cement mortar but also changed the morphology of cement hydration products. As shown in Figures 3.26(c) and 3.26(d), after EICI treatment, the cement mortars featured denser and more compact microstructure, which is likely attributed to the chemical and physical binding of [TBA+] to the C-S-H gel and other cement hydrates. These physicochemical changes in the mortars after the EICI treatment are likely responsible for the observed increases in their compressive strength (as seen in Figure 3.26).

3.3. Application of ECE and EICI methods for rehabilition of chloride-contaminated reinforced concrete

## 3.3.3. On site trial at Lan 1-watergate (Tien Hai, Thai Binh)

Figure 3.41 shows the position-column reinforced concrete (1 metre in length) at the on- site application. The electrolytic storage material made by polyester and cellulose fibers. In ECE procedure, the electrolyte was 0,1M Na3BO3 and current density was 1A/m2. The ECE duration was 15 days. After ECE termination, EICI was then applied by adding TBAB into the electrolyte (at 25 mM of concentrtion). The EICI current density was 5A/m2. The EICI duration was 30 days. The testing data after ECE and EICI treatments were listed in Table 3.13.

.

# Figure 3.41: On site application at Lan 1-Watergate (Thai Binh)

As can be seen in Table 3.13, the ECE/EICI treatments have successfully rehabilitated the contaminated reinforced concrete in the coastal area. The protecting performance was also observed after 1 year from the termination of treatment (OCP varied arround -118 mV/SCE).

Table 3.13: Values of chloride and [TBA+] concentrations, OCP of rebar: before and after ECE/EICI treatment at Lan 1-Watergate

| Method | Time (wks) | Chlorid (wt% .) |  | [TBA+] (wt.% ) |  | Eoc (mV/SCE) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Before | After | Before | After | Before | After (months) |  |
|  |  |  |  |  |  |  | 2 | 12 |
| ECE | 2 | 0,89 | 0,17 | 0 | 0 | -350 | NA | NA |
| EICI | 4 | 0,17 | 0,19 | 0 | 1,94 | NA | -70 | -118 |

Conclusion of 3.3 part

Establish the system and electrolytic storage material for the on-site trial of ECE and EICI methods for chloride contaminated concrete structure at Lan 1- Water gate (ThaiBinh). After 2 weeks ECE, 81,2% chloride content was removed from the position column. After 4 weeks EICI, [TBA+] concentration around rebar reached at  the value of 2,2 wt.%. After 1 year (since the disconnection of test), the rebar was still in the passive state under good protection.

# CONCLUSION

The main findings of this investigation include:

- ECE treatment was effective in removing chlorides whenusing both electrolytes. Chloride content was decreased by70% relative to the initial chloride after 4 weeks of treatment. When using a current density of 1 A/m2, the chloride reduction increased with increasing time of treatment.The potentiodynamic weak polarization tests showed thatECE treatment halted chloride-induced corrosion of therebar by passivating it. If a current density of 1 A/m2 was usedduring the ECE, the values of  icorr after 4 weeks decreased by 36 and 34 per cent, respectively. The EIS data revealed that ECE treatment increased theresistivity of the mortar, leading to the formation of a more dense and less permeable microstructure of cement mortars. ECE treatment improved significantly the compressive strength of the mortar..

- After 4-week EICI treatment in NaOH, [TBA+] content was 2.0% and 2.5% by mass of cement mortar, for uncontaminated and chloridecontaminatedsamples, respectively. The potentiodynamic weak polarization tests showed that EICI treatment halted chloride-induced corrosionof the rebar. The electromigration test showed that EICI improved the chloride penetration resistanceof the mortar, as indicated by the reduced apparentdiffusion coefficients of chloride anion, by 38%from 1.0 × 10−10 m2/s. EICI treatmentsignificantly improved the compressive strength ofcement mortars.

-	Establish the system and electrolytic storage material for the on-site trial of ECE and EICI methods for chloride contaminated concrete structure at Lan 1- Water gate (ThaiBinh). After 2 weeks ECE, 81,2% chloride content was removed from the position column. After 4 weeks EICI, [TBA+] concentration around rebar reached at the value of 2,2 wt.%. After 1 year (since the disconnection of test), the rebar was still in the passive state under good protection.

# Novelty and contribution of thesis

- Study and application of EICI method for injection of corrosion inhibitor into the reinforced structure in Vietnam. [TBA+] ions were injected at the content of 1.5 to 2 wt.% (by weight of cement motar) near the rebar (at distance of 1 cm). The potentiodynamic weak polarization tests showedthat EICI treatment halted chloride-induced corrosionof the rebar. The electromigration test showed that EICI improved the chloride penetration resistanceof the mortar, as indicated by the reduced apparentdiffusion coefficients of chloride anion, by 38%from 1.0 × 10−10 m2/s. EICI treatmentsignificantly improved the compressive strength ofcement mortars.

- Application of ECE and EICI method to rehabilitate a part of chloride-contaminated  reinforced concrete  structure at Lan 1- Water gate (ThaiBinh). After 2 weeks ECE, 81,2% chloride content was removed from the position column. After 4 weeks EICI, [TBA+] concentration around rebar reached at  the value of 2,2 wt.%. After 1 year (since the disconnection of test), the rebar was still in the passive state under good protection.